|  | Aura Luxpro Remix Anticor Anticorrosive Acrylic Enamel Straight on rust Reliable metal protection Water-based Odorless Quick drying |
| --- | --- |
| Description |
| Properties | Anticorrosive acrylic water-based enamel. Acrylic water-based. Odorless. Ready to use. Does not require advance priming. It contains a rust converter and anti-corrosion components. Can be applied to ferrous metals with remnants of tightly held rust with a thickness of up to 70 microns and scale. Provides reliable protection against corrosion and weathering. Passivates the surface of the metal, stops corrosion damage. If the coating is damaged, rust is formed only on an unprotected surface, not spreading under the Remix Anticor membrane. Durable, weatherproof. Forms a matte membrane that visually conceals minor surface irregularities. Quick drying. When applied it does not form harmful, unpleasant and flammable vapors. Good adhesion (adhesion force) to the surface to be painted. Primer-enamel Remix Anticor can be painted on surfaces previously painted with enamels or varnishes: alkyd, acrylic, urethane, organosilicon. Does not contain organic solvents, as well as lead, chromium, mercury and other carcinogenic substances. |
| Purpose | For anticorrosive protection and decorative painting of ferrous metal surfaces (steel, cast iron), which are used in atmospheric conditions. Attention! Remix Anticor enamel is not intended for painting galvanized surfaces. |
| Types of surfaces for drawing | Recommended for painting: forged products, garages, gates, fences, grilles, garden metal furniture, heating radiators, household building structures, etc. Remix Anticor can be used to protect industrial structures and equipment when operating in non-corrosive environments. For exterior and interior. |
| Quality standards | 1 wear class according to DIN EN 13300. VOC content (volatile organic compounds) complies with European Union directive 2004/42 / CE. |
| Specifications |
| Surface preparation | The surface must be dry and durable. Before painting the metal surface must be mechanically cleaned from loose and fragile layer of rust and unstable scale, dirt, oil, grease, dust, etc. Remove the peeling paint from the previously painted surface. To degrease and dry the surface. Smooth surfaces to roughen. |
| Drawing | Stir before use. Apply with a brush, roller, spray gun. When applied with a brush, roller - do not dilute. When sprayed, if necessary, it can be diluted with water to no more than 5% by volume to a working viscosity. It is recommended to apply at a temperature of surface, primer-enamel, air + 18 ± 2 ºС and relative humidity of air 65 ± 5%. Do not apply at temperatures below + 5ºС and above + 30ºС. To achieve consumer properties, Remix Anticor must be applied with interlayer drying 60 ± 10 minutes: in 2 layers for internal surfaces; in 3 layers for exterior surfaces. To create a reliable protective coating, the thickness of the dry paint membrane should be: - 80 microns for interior work (when applied in 2 layers with a flow rate of up to 9.5 m2 / l per layer); - 120 microns for outdoor use (when applied in 3 layers with a flow rate of up to 9.5 m² / l per layer). When using Remix Anticor in industrial technology – ask for manufacturer's recommendations! |
| Care of the painted surface | Do not use abrasive detergents or hard sponges to clean the surface. If abraded, the surface may become glossy. |
| Color | Ready colors according to the catalog: white, black (RAL 9011), dark gray (RAL 7043), red-brown (RAL 8012), dark brown (RAL 8017), blue (RAL 5005), green (RAL 6005), red (RAL 3016), yellow (RAL 1018). |
| Consumption | Up to 9.5 m²/l undiluted primer enamel per one coat. Consumption depends on the color, type and surface preparation, the color of the primer-enamel. |
| Drying time | At a temperature of + 20ºС and relative air humidity of 65%: 30 minutes from dust; 60 ± 10 minutes - applying the next layer; 24 hours - resistant to weathering; 20 days - a complete set of strength. Drying time depends on the temperature, relative humidity of the air, and the thickness of the paint film. With decrease in temperature and increase in humidity, the drying time increases. |
| Tools | Brush, roller, spray. |
| Cleaning tools | Immediately after work, rinse with warm water and detergent. When dry, clean mechanically or with organic solvents. |
| Composition | Acrylic dispersion, anticorrosive pigments, fillers, rust converters, water, special additives. |
| Additional Information |
| Frost resistance | Do not freeze during storage. |
| Warranty period of storage | 24 months from the date printed on the package. |
| Storage conditions | Store and transport in intact original tightly closed packaging at a temperature from + 5 ° C to + 35 ° C. Protect from freezing, heating devices and direct sunlight. |
| Precautionary measures | During the work follow the general rules of occupational health. The material is eco-friendly, fire and explosion safe. Keep out of reach of children. Work in a ventilated area. Avoid contact with eyes and skin. In case of contact with eyes or skin, rinse with water. Rubber gloves should be used to protect hands; eye glasses should be used, and a respirator should be used when painting with a paint sprayer. Do not breathe mist when spraying. |
| Recycling | Do not pour into drains, water bodies, on the ground. Dispose of dry product and container as household waste. |
| Volume / weight | 0.75 L (0.9 kg); 2.2 L (2.6 kg) |
| The information concerning the product is based on the results of laboratory tests and practical use of the product depending on the location and conditions of its use. As the manufacturer, we guarantee the quality of the product and provide the best recommendations for its appropriate application. As the manufacturer, we cannot control the conditions and circumstances of product transportation, storage and application and numerous other factors that affect its use. Thus, we shall not bear responsibility for the damage caused by ignoring the instructions for use or transportation, by noncompliance with storage conditions and timeframes or by inappropriate application of the product. The manufacturer reserves the right to alter product information at their discretion without prior notice. For additional information, please contact us: http://eskaro.ua/ |
| Redaction Technical Specifications. № 02 dated 11/03/2019. |